Durban

Manufacturing process

1/10” loop pile

Pile content

60 % PA/ 40 % PP

Primary backing

Twinback

Pile weight

± 660 gr./m²

Total weight

± 1.800 gr./m²

Pile height

± 3 mm

Total height

± 7 mm

Tuft density/m²

± 225 000

Width

400 + 500 cm

Sound insulation

± 22 dB

Fire class

Cfl-s1 (EN 13501-1)

only with full adhesion