Florida

****

Manufacturing process

**1/10” Tufted loop pile**

Pile content

**60 % PA / 40 % PP**

Primary backing

**Bitumen**

Pile weight

**ca. 660 gr./m²**

Total weight

**ca. 4.050 gr./m²**

Pile height

**ca. 3 mm**

Total height

**ca. 6 mm**

Tuft density/m²

**ca. 215 000**

Size

**50 x 50 cm**





